(Note to Specifier:  This specification has additional instructions included as Hidden Text.  To view this information, Select Tools, Options, and check Hidden Text in the Formatting Marks section of the View Tab.)

# 2004 MASTER FORMAT™ SECTION 09 840

Acoustical Wall Treatment

Hush Clad

GENERAL

RELATED DOCUMENTS

Drawings and general provisions of the Contract, including General and Supplementary Conditions and other Division 1 Specification sections, apply to this Section.

summary

This Section includes the Acoustic Finishes as shown and specified in the described system(s): Adjust list below to suit Project

Wall Acoustic Finish

Ceiling Acoustic Finish

Feature Wall

[Insert Item]

Related Sections include the following:

Adjust list below to suit Project

Section 09800 Acoustical Treatment, 098000 Acoustical Treatment, 09810 Acoustical Space Unit, 098300 Acoustic Finishes

Section 09700 Wall Finishes, 09710 Acoustical Wall Finishes, 09720 Wall Covering

Section 09521 Acoustical Ceiling Wall Panels

submittals

General:  Submit the following in accordance with conditions of contact and Division 1 specification section 01 33 00 “Submittal Procedures”.

Product Data:  Submit manufacturer’s product data; include product description, fabrication information, and compliance with specified performance requirements.

Submit product test reports from a qualified independent 3rd party testing agency indicating each type and class of panel system complies with the project performance requirements, based on comprehensive testing of current products.  Previously completed test reports will be acceptable if for current manufacturer and indicative of products used on this project.

Test reports required are:

Steiner Tunnel Surface Burning Rate Test (ASTM E 84)

ASTM C423

Dynamic environmental testing (ASTM standards D 5116 and D 6670)

Shop Drawings:  Include plans, elevations, sections, panel dimensions, details, and attachments to other work.

Samples for Initial Selection:

Submit minimum 2-inch by 2-inch samples.  Indicate full color and pattern.

Samples for Verification:

Submit minimum 4-inch by 4-inch sample for each color

Delete below if mockups are not required

Mockups:

Build mockups to verify selections made under sample Submittals and to demonstrate aesthetic effects.

Build mockup of [each type of] Acoustic Finish.

Retain subparagraph below if mockups are erected as part of building rather than separately

Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Maintenance Data:  Submit manufacturer’s care and maintenance data, including care, repair and cleaning instructions.  Include in Project closeout documents.

quality assurance

Manufacturers Qualifications

Materials and systems shall be manufactured by a company continuously and regularly employed in the manufacture of specified materials for a period of at least two (2) consecutive years and which can show evidence of those materials being satisfactorily used on at least three (3) projects of similar size, scope and location.  At least three (2) of the projects shall have been successful for use two (2) years or longer.

Manufactured panels must be produced from a minimum of 50% post-industrial recycle content.

Manufacturer must offer a documented reclaim process that will take back, at the manufacturers cost, panels that are at their end-of life cycle.  Return process is preceded by following requirements highlighted in Section 02 42 00 Removal and Salvage of Construction Materials.

delivery, storage, and handling

Deliver Acoustic Finishes and specified items in manufacturer’s standard protective packaging.

Do not deliver Acoustic Finishes, components and accessories to Project site until areas are ready for installation.

Store materials in a flat orientation in a dry place that is not exposed to exterior elements.

Handle materials to prevent damage to finished surfaces.  Provide protective coverings to prevent damage or staining following installation for duration of project.

Before installing Acoustic Finishes, permit them to reach room temperature.

Project Conditions

Environmental Limitations:  Do not install Acoustic Finishes until spaces are enclosed and weatherproof, and ambient temperatures and humidity conditions are maintained at the levels indicated for Project when occupied for its intended use.

Warranty

Manufacturer’s Special Warranty on polymer panel system:  Manufacturer’s standard form agreeing to repair or replace units that fail in material or workmanship within the specified warranty period.

Warranty Period:  1 year after the date of substantial completion.

The warranty shall not deprive the owner of other rights or remedies the Owner may have under other provisions of the Contract Documents, and is in addition to and runs concurrent with other warranties made by the Contractor under the requirements of the Contract Documents.

PRODUCTS

Manufacturer

Manufacturer:  3form, LLC., Salt Lake City, Utah, USA / Telephone 801-649-2500

Materials

Hush Clad produced from Sola Felt

Recycled Rigid PET Felt

Size: Various

Thickness: Sola Felt 3/8”

Basis of Design Product:  The design of Acoustic Tile systems is provided by 3form, LLC.  Products from other manufacturers must be approved by the Architect or Designer prior to bidding in accordance with the Instructions to Bidders and Section 10 60 00 “Product Requirements”.

Sheet minimum performance attributes:

Noise Reduction Coefficient (ASTM C423) – 0.35

Dynamic environmental testing (ASTM standards D 5116 and D 6670).  Panels must not have detectable VOC off-gassing agents and must be have Greenguard™ Indoor Air Quality certified.

Panels must be produced from a minimum of 50% post-industrial recycle content.

Miscellaneous Materials

General: Provide products of material, size, and shape required for application indicated, and with a proven record of compatibility with surfaces contacted in installation.

Cleaner:  Type recommended by manufacturer.

EXECUTION

examination

Examine substrates, areas, and conditions where installation of Acoustic Finishes will occur, with Installer present, for compliance with manufacturer’s requirements.  Verify that substrates and conditions are satisfactory for installation and comply with requirements specified.

installation

General:  Comply with manufacturer’s written instructions for the installation of Acoustic Finishes.

Utilize fasteners provided by manufacturer.

Install components plumb, level and rigid, scribed to adjacent finishes, in accordance with approved shop drawings and product data.

We recommend that installation is completed by a 3form Certified Installer. Contact 3form for more information or to get a quote.

cleaning and protection

Protect surfaces from damage until date of substantial completion.  Repair work or replace damaged work, which cannot be repaired to Architect’s satisfaction.

# End of Section 09 840

# Product:	[Replace with Pattern]

Color:	[Replace with color name]

Gauge:	[3/8"]

Surface Finish:	[Standard]

UV Protection is desirable for applications that will receive direct sunlight.

# Installation Type: 	[Wall][Ceiling]

Refer to www.3-form.com for expansion/contraction information.  This information is required for applications subjected to temperature variation.

Repeat Product Data Sheets as required to identify all Varia™ applications.