(Note to Specifier:  This specification has additional instructions included as Hidden Text.  To view this information, Select Tools, Options, and check Hidden Text in the Formatting Marks section of the View Tab.)

2004 MASTER FORMAT™ SECTION 06 06 60

Schedules for Plastic Fabrications

3form Edge System

GENERAL

RELATED DOCUMENTS

Drawings and general provisions of the Contract, including General and Supplementary Conditions and other Division 1 Specification sections, apply to this Section.

summary

This Section includes the Plastic Fabrications as shown and specified in the described system(s): Adjust list below to suit Project

Ceiling Panels

Feature Wall

Wall Cladding

Wall Cladding-back-lit

Wall Panels-back-lit

Wall Sculpture

Partitions

[Insert Item]

Related Sections include the following:

Adjust list below to suit Project

Section 06 06 60 Schedules for Plastic Fabrications; Section 06 06 70 Schedules for Structural Composites; Section 06 06 80 Schedules for Composite Assemblies

Section 09 54 00 Specialty Ceiling;

Section 10 11 00 Visual Display Surfaces; Section 10 21 00 Compartments and Cubicles;

submittals

General:  Submit the following in accordance with conditions of contact and Division 1 specification section 01 33 00 “Submittal Procedures”.

Product Data:  Submit manufacturer’s product data; include product description, fabrication information, and compliance with specified performance requirements.

Submit product test reports from a qualified independent 3rd party testing agency indicating each type and class of panel system complies with the project performance requirements, based on comprehensive testing of current products.  Previously completed test reports will be acceptable if for current manufacturer and indicative of products used on this project.

Test reports required are:

Rate of Burning (ASTM D 635)

Self-Ignition Temperature (ASTM D 1929)

Density of Smoke (ASTM D 2843)

Room Corner Burn Test (NFPA 286)

Extent of Burning (UL 94)

Impact strength (ASTM D 3763)

Safety glazing impact resistance (ANSI Z97.1-2004)

UPITT Test for Combustion Product Toxicity

Dynamic environmental testing (ASTM standards D 5116 and D 6670)

Building Approvals:  Plastic Fabrications are to have been evaluated and must be registered with and comply to requirements of the following jurisdictions:

Los Angeles Department of Building and Safety (Product must have a LARR [Los Angeles Research Report] number) for use as Light-transmitting Panels

Shop Drawings:  Include plans, elevations, sections, panel dimensions, details, and attachments to other work.

Samples for Initial Selection:

Submit minimum 2-inch by 2-inch samples.  Indicate full color, texture and pattern variation.

Samples for Verification:

Submit minimum 4-inch by 4-inch sample for each color of Plastic Fabrications

Delete below if mockups are not required

Mockups:

Build mockups to verify selections made under sample Submittals and to demonstrate aesthetic effects.

Build mockup of [each type of] Plastic Fabrications.

Retain subparagraph below if mockups are erected as part of building rather than separately

Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

Maintenance Data:  Submit manufacturer’s care and maintenance data, including care, repair and cleaning instructions.  Include in Project closeout documents.

quality assurance

Manufacturers Qualifications

Materials and systems shall be manufactured by a company continuously and regularly employed in the manufacture of specified materials for a period of at least two (2) consecutive years and which can show evidence of those materials being satisfactorily used on at least three (3) projects of similar size, scope and location.  At least three (2) of the projects shall have been successful for use two (2) years or longer.

Manufactured panels must be produced from a minimum of 40% post-industrial recycle content.  This recycle content must be certified by a recognized 3rd party certification group, such as Scientific Certification Systems (SCS).

Manufacturer must offer a documented reclaim process that will take back, at the manufacturers cost, panels that are at their end-of life cycle.  Return process is preceded by following requirements highlighted in Section 02 42 00 Removal and Salvage of Construction Materials.

delivery, storage, and handling

Deliver Plastic Fabrications and specified items in manufacturer’s standard protective packaging.

Do not deliver Plastic Fabrications, components and accessories to Project site until areas are ready for installation.

Store materials in a flat orientation in a dry place that is not exposed to exterior elements.

Handle materials to prevent damage to finished surfaces.  Provide protective coverings to prevent damage or staining following installation for duration of project.

Before installing Plastic Fabrications, permit them to reach room temperature.

Project Conditions

Environmental Limitations:  Do not install Plastic Fabrications until spaces are enclosed and weatherproof, and ambient temperatures and humidity conditions are maintained at the levels indicated for Project when occupied for its intended use.

Warranty

Manufacturer’s Special Warranty on polymer panel system:  Manufacturer’s standard form agreeing to repair or replace units that fail in material or workmanship within the specified warranty period.

Warranty Period:  1 year after the date of substantial completion.

The warranty shall not deprive the owner of other rights or remedies the Owner may have under other provisions of the Contract Documents, and is in addition to and runs concurrent with other warranties made by the Contractor under the requirements of the Contract Documents.

PRODUCTS

Manufacturer

Manufacturer:  3form, Inc., Salt Lake City, Utah, USA / telephone 801-649-2500

Materials

Edge produced from Varia Ecoresin® Sheet

Engineered polyester resin

Fin Size: Various, between 3” -13” wide x 96” high

Panel size (for yield): 48” x 96”

Thickness: 1/4”

Basis of Design Product:  The design of plastic panel systems is based on Edge produced with Varia Ecoresin® as provided by 3form, Inc.  Products from other manufacturers must be approved by the Architect or Designer prior to bidding in accordance with the Instructions to Bidders and Section 10 60 00 “Product Requirements”.

Interlayer Materials:  Compatible with polyesters and bonding process to create a monolithic sheet of material when complete.

Sheet minimum performance attributes:

Rate of Burning (ASTM D 635).  Material must attain CC1 Rating for a nominal thickness of 6 mm (0.250 in.) and greater.

Self-Ignition Temperature (ASTM D 1929).  Material must have a Self-ignition temperature greater than 650°F.

Density of Smoke (ASTM D 2843).  Material must have a smoke density less than 75%.

Room Corner Burn Test (NFPA 286).  Material must meet Class A criteria at ¼” thickness as described by the 2003 International Building Code.

Extent of Burning (UL 94).  Must submit UL card.

Impact strength. Minimum impact strength test as measured by ASTM D 3763 of 20 ft. lbs.  (for durability, shipping, installation, and use).

Safety Glazing.  Material must attain a Class A impact rating in accordance with ANSI Z97.1-2004 at 1/8” thickness.

UPITT Test for Combustion Product Toxicity:  Product must be recorded as “not more toxic than wood”.

Dynamic environmental testing (ASTM standards D 5116 and D 6670).  Panels must not have detectable VOC off-gassing agents and must be have Greenguard™ Indoor Air Quality certified.

Panels must be produced from a minimum of 40% post-industrial recycle content.  This recycle content must be certified by a recognized 3rd party certification group, such as Scientific Certification Systems (SCS).

Building Approvals:  Plastic Fabrications are to have been evaluated and must be registered with and comply to requirements of the following jurisdictions:

Los Angeles Department of Building and Safety (Product must have a LARR [Los Angeles Research Report] number) for use as Light-transmitting Panels

Miscellaneous Materials

General: Provide products of material, size, and shape required for application indicated, and with a proven record of compatibility with surfaces contacted in installation.

Cleaner:  Type recommended by manufacturer.

Railing System:  Use included hardware specifically designed for 3form Edge.

Bonding Cements: May be achieved with solvents or adhesives, suitable for use with product and application.

EXECUTION

examination

Examine substrates, areas, and conditions where installation of Plastic Fabrications will occur, with Installer present, for compliance with manufacturer’s requirements.  Verify that substrates and conditions are satisfactory for installation and comply with requirements specified.

installation

General:  Comply with manufacturer’s written instructions for the installation of Plastic Fabrications.

Utilize fasteners provided by manufacturer.

Install components plumb, level and rigid, scribed to adjacent finishes, in accordance with approved shop drawings and product data.

We recommend that installation is completed by a 3form Certified Installer. Contact 3form for more information or to get a quote.

cleaning and protection

Protect surfaces from damage until date of substantial completion.  Repair work or replace damaged work, which cannot be repaired to Architect’s satisfaction.

End of Section 06 06 60

Solid Polymer Fabrication #1 (SPF-1)

Product:	[Replace with Collection and product name]

Color:	[Replace with color name]

Gauge:	[1/4"]

Surface Finish:	[Sandstone]

UV Protection is desirable for applications that will receive direct sunlight.

UV Protection: 	[required][not required]

Edge Sealing: 	[required][not required]

Installation Type: 	[Wall][Partition][Ceiling]

Refer to www.3-form.com for expansion/contraction information.  This information is required for applications subjected to temperature variation.

Repeat Product Data Sheets as required to identify all Varia™ applications.